# FWPCOT2217 Visually stress grade cypress

Release: 1

FWPCOT2217 Visually stress grade cypress

# Modification History

| Release | Comment |
| --- | --- |
| 1 | Replaces equivalent unit FPICOT2217B Visually stress grade cypress, which was first released with FPI11 Forest and Forest Products Training Package Version 1. This is the first release of this unit in the new standards format. |

# Application

This unit of competency describes the outcomes required to visually stress grade Australian white cypress (Callitris glaucophylla) by assessing material for strength against set classifications as detailed in Section 3 of the Australian Standard AS2858 as a minimum standard.

The unit applies to those who visually stress-grade cypress in a forest products factory setting.

No licensing, legislative, regulatory, or certification requirements apply to this unit at the time of publication.

# Pre-requisite Unit

Nil

# Unit Sector

Sawmilling and Processing

Timber Manufactured Products

Wood Panel Products

# Elements and Performance Criteria

| ELEMENTS | PERFORMANCE CRITERIA |
| --- | --- |
| Elements describe the essential outcomes. | Performance criteria describe the performance needed to demonstrate achievement of the element. Where bold italicised text is used, further information is detailed in the range of conditions. |
| 1. Prepare for stress-grading | 1.1 Review work order for visually stress-grading cypress and clarify with appropriate personnel. 1.2 Identify grading requirements in line with site procedures, standards and specifications. 1.3 Select materials, hardware items, tools and equipment appropriate to work order and check for operational effectiveness. 1.4 Position cypress to be graded to provide appropriate access and facilitate efficient workflow. 1.5 Establish and maintain communication with others at site to ensure safety. |
| 2. Evaluate cypress | 2.1 Identify species and check status of seasoning. 2.2 Accurately record size and tolerance measurements in line with site requirements. 2.3 Establish characteristics and evaluate in line with standards and product specifications. 2.4 Measure moisture content and evaluate against standards and seasoning requirements. |
| 3. Grade cypress | 3.1 Visually stress grade cypress based on standards for the required structural grade. 3.2 Diagnose and check characteristics with the greatest limiting effect on the grade. 3.3 Assess the appearance, and mark, segregate and dispose of, in line with site procedures and environmental requirements 3.4 Record and report results of grading in line with workplace procedures. |

# Foundation Skills

| This section describes those core and employment skills that are essential to performance and are not explicit in the performance criteria. |  |
| --- | --- |
| Numeracy skills to: | estimate, measure and calculate sizes of cypress effectively calibrate and use moisture meter. |
| Writing skills to: | accurately compile and complete grading reports. |

# Range of Conditions

Not Applicable

# Unit Mapping Information

FPICOT2217B Visually stress grade cypress

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=0d96fe23-5747-4c01-9d6f-3509ff8d3d47