# FWPSAW3247 Replace tungsten tips

Release: 1

FWPSAW3247 Replace tungsten tips

# Modification History

| Release | Comments |
| --- | --- |
| Release 1 | This version released with FWP Forest and Wood Products Training Package Version 5.0. |

# Application

This unit of competency describes the skills and knowledge required to remove worn or damaged tungsten tips from circular saw blades, and braze, clean and prepare replacement tips for grinding and return to service.

The unit applies to individuals who replace tungsten tips in a saw technician workshop or timber processing facility.

All work must be carried out to comply with workplace procedures, according to state/territory health and safety regulations, legislation and standards that apply to the workplace.

No licensing, legislative or certification requirements apply to this unit at the time of publication.

# Pre-requisite Unit

Nil

# Unit Sector

Sawmilling and Processing (SAW)

# Elements and Performance Criteria

| Elements | Performance Criteria |
| --- | --- |
| Elements describe the essential outcomes. | Performance criteria describe the performance needed to demonstrate achievement of the element. |
| 1. Prepare for replacement | 1.1 Review work order to determine job requirements and, where required, seek clarification from appropriate personnel 1.2 Review workplace health and safety procedures, including the use of personal protective equipment, equipment lock-out and safe manual handling techniques 1.3 Identify, assess and take actions to mitigate risks and hazards associated with replacing tungsten tips 1.4 Identify workplace environmental protection procedures for minimising and disposing of waste material, cleaning tools and equipment, and maximising energy efficiency 1.5 Select appropriate tools and equipment, and check for operational effectiveness according to manufacturer recommendations |
| 2. Remove worn, damaged or broken tips | 2.1 Remove and replace saw blade according to manufacturer instructions 2.2 Assess saw blade condition 2.3 Clean foreign matter from saw and check for defects 2.4 Identify and mark broken tips 2.5 Remove broken tips, minimising damage to the tooth seat, and dispose of according to environmental protection practices 2.6 Repair tooth seats to specified tolerance and dimensions |
| 3. Replace tips | 3.1 Set up saw in brazing jig according to manufacturer instructions 3.2 Select brazing material and suitable technique for application and heat control 3.3 Select appropriate replacement tip and braze into position 3.4 Trial braze one tip, check tip is correctly positioned and the silver alloy has flowed evenly to both sides of the tip 3.5 Inspect and verify tip position, side clearance, and joint quality objectives have been achieved 3.6 Set manual or automatic feeds according to number of tips to be brazed 3.7 Identify routine processing and equipment faults, and resolve or report to appropriate personnel |

# Foundation Skills

This section describes those language, literacy, numeracy and employment skills that are essential for performance in this unit of competency but are not explicit in the performance criteria.

| Skill | Description |
| --- | --- |
| Numeracy | Uses standard units of measurement and symbols for temperature and volume Uses basic arithmetic skills to determine amount of brazing material required when replacing tips |
| Navigate the world of work | Understands main tasks, responsibilities and boundaries of own role |
| Interact with others | Uses modes of communication suitable to purpose to confirm and clarify understanding |
| Get the work done | Recognises and responds to routine problems |

# Unit Mapping Information

| Code and title current version | Code and title previous version | Comments | Equivalence status |
| --- | --- | --- | --- |
| FWPSAW3247 Replace tungsten tips | FWPSAW3218 Replace tungsten tips | Renamed element; updated performance criteria; revised performance evidence for clarity; updated knowledge evidence | Equivalent unit |

# Links

Companion Volumes, including Implementation Guides, are available at VETNet: - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=0d96fe23-5747-4c01-9d6f-3509ff8d3d47

Assessment Requirements for FWPSAW3247 Replace tungsten tips

# Modification History

| Release | Comments |
| --- | --- |
| Release 1 | This version released with FWP Forest and Wood Products Training Package Version 5.0. |

# Performance Evidence

An individual demonstrating competency must satisfy all of the elements and performance criteria in this unit.

There must be evidence that, on at least one occasion, the individual has:

followed work order and relevant workplace health and safety and environmental protection procedures

removed worn tungsten tips from circular saw blades

replaced tungsten tips for circular saw blades

assessed condition of tungsten tips in line with workplace procedures.

# Knowledge Evidence

An individual must be able to demonstrate the knowledge required to perform the tasks outlined in the elements and performance criteria of this unit. This includes knowledge of:

basic knowledge of physics of sawing, including:

saw blade material and properties

impact of timber properties on saw blades

direction of cut

forces on a blade

heat removal

saw tooth configuration

purpose, features and operation of saws for which tungsten tips are replaced:

circular saws

features and names of different parts of saw blades

purpose, features and operation of tools and equipment used to replace tungsten tips:

brazing equipment and brazing material

brazing jigs

methods for:

removing saw blades from saws

assessing saw blade condition

removing tungsten tips from saw blades

cleaning excess braze alloy and carbide fragments from tip seats

lengthening or deepening tip seats to match replacement tip requirements

selecting size and type of replacement tip

pre-tinning new tips

brazing new tungsten tips onto the tooth face or tooth seat

appropriate tolerances for brazing alloy joint thickness, replacement tip sizes and side clearance objectives

characteristics of metal used in saw blades, and effects of brazing

types of risk and hazards and mitigation measures associated with replacing tungsten tips

workplace procedures specific to replacing tungsten tips:

workplace health and safety, with particular emphasis on equipment lock-out and use of personal protective equipment (PPE)

communication reporting lines

recording and reporting processing and equipment faults

environmental protection practices applicable to saw technician workshops or timber processing facilities:

reducing water and energy use

cleaning plant, tools and equipment

disposing of, recycling and reusing materials.

# Assessment Conditions

Assessment of skills must take place under the following conditions:

physical conditions:

skills must be demonstrated in a saw technician workshop, timber processing facility or an environment that accurately represents workplace conditions

resources, equipment and materials:

brazing equipment

brazing jigs

circular saws

tungsten tips

brazing material: silver alloy, flux in the form of a liquid or paste

side clearance dial indicator: Kafer Gauge

PPE suitable for replacing tungsten tips

specifications:

documents, spreadsheets and templates for recording operation and equipment faults

manufacturer instructions for use, repair and maintenance of equipment

work order with specific instructions for replacing tungsten tips for circular saws

workplace procedures for replacing tungsten tips.

Assessors of this unit must satisfy the requirements for assessors in applicable vocational education and training legislation, frameworks and/or standards.

# Links

Companion Volumes, including Implementation Guides, are available at VETNet: - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=0d96fe23-5747-4c01-9d6f-3509ff8d3d47