# MEM04025 Produce moulds and cores by hand (advanced)

Release: 2

MEM04025 Produce moulds and cores by hand (advanced)

# Modification History

Release 2. Quantum of hours of workplace practice removed. Supersedes and is equivalent to MEM04025 Produce moulds and cores by hand (advanced) (Release 1).

Release 1. Supersedes and is not equivalent to MEM04005C Produce moulds and cores by hand (jobbing).

# Application

This unit of competency has been developed for Engineering Tradesperson – Casting and Moulding apprenticeship training and the recognition of trade-level skills in the production of moulds and cores using advanced manual (jobbing) methods. It defines the skills and knowledge required to use advanced manual (jobbing) methods to produce moulds and cores for the production of metal castings and includes the ability to match patterns, moulds and cores to meet requirements.

Where the selection and use of welding skills is required unit MEM05012 Perform routine manual metal arc welding and unit MEM05050 Perform routine gas metal arc welding, should also be selected as appropriate.

Where lifting and moving moulds and cores requires the use of mobile load shifting equipment or overhead cranes, appropriate manual handling units should also be selected.

No licensing, legislative or certification requirements apply to this unit at the time of publication.

Band:	A

Unit Weight:	12

# Pre-requisite Unit

| MEM04024 | Produce moulds and cores by hand |
| --- | --- |
| MEM09002 | Interpret technical drawing |
| MEM11011 | Undertake manual handling |
| MEM12023 | Perform engineering measurements |
| MEM12024 | Perform computations |
| MEM13015 | Work safely and effectively in manufacturing and engineering |
| MEM14006 | Plan work activities |
| MEM16006 | Organise and communicate information |
| MEM18001 | Use hand tools |
| MEM18002 | Use power tools/hand held operations |

# Competency Field

Casting and moulding

# Elements and Performance Criteria

| Elements describe the essential outcomes. |  | Performance criteria describe the performance needed to demonstrate achievement of the element. |  |
| --- | --- | --- | --- |
| 1 | Determine job requirements | 1.1 | Follow standard operating procedures (SOPs) |
|  |  | 1.2 | Comply with work health and safety (WHS) requirements at all times |
|  |  | 1.3 | Use appropriate personal protective equipment (PPE) in accordance with SOPs |
|  |  | 1.4 | Identify job requirements from specifications, drawings, job sheets or work instructions |
|  |  | 1.5 | Determine sequence of operations, including material selection, job set up, for maximum safety, efficiency and to meet job specifications |
| 2 | Select inspect and prepare pattern equipment | 2.1 | Identify pattern and associated equipment from specifications |
|  |  | 2.2 | Inspect pattern equipment conformance to specifications, and identify damaged patterns for repair or replacement |
|  |  | 2.3 | Assemble pattern to specification |
|  |  | 2.4 | Set up pattern equipment to specification |
| 3 | Make mould and core | 3.1 | Position core in prints utilising chaplets and chills, as required, and vent to specification |
|  |  | 3.2 | Close mould and check for compliance to component specification |
|  |  | 3.3 | Select and position appropriate moulding/core making equipment |
|  |  | 3.4 | Select and use appropriate moulding media to produce mould and core to specification |
|  |  | 3.5 | Secure mould |
|  |  | 3.6 | Select or manufacture pouring basin to specification and position in accordance with procedures |
|  |  | 3.7 | Ram up mould and cores with joints and drawbacks as required |
|  |  | 3.8 | Use parting and stripping systems |
|  |  | 3.9 | Position and secure loose pieces, vents, risers and runners as required |
|  |  | 3.10 | Remove pattern and loose pieces from mould and core box in safely and without causing damage to the pattern |
|  |  | 3.11 | Inspect and repair mould as required |
|  |  | 3.12 | Clean and paint mould and core according to specification using site procedures |
| 4 | Complete work requirements | 4.1 | Leave the worksite in a safe state, including clearing all materials/debris and cleaning the worksite |
|  |  | 4.2 | Dispose of unwanted treated sand according to SOPs |
|  |  | 4.3 | Complete reports/records in accordance with SOPs |

# Foundation Skills

This section describes those required skills (reading, writing, oral communication and numeracy) that are essential to workplace performance in this unit of competency.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Range of Conditions

| This field allows for different work environments and conditions that may affect performance. Essential operating conditions that may be present (depending on the work situation, needs of the candidate, accessibility of the item, and local industry and regional contexts) are included. |  |  |
| --- | --- | --- |
| Materials include one (1) or more of the following: | binders hardeners sand additives mould coatings |
| Patterns include one (1) or more of the following: | irregular/uneven patterns with undercuts multi-joint consumable loose piece patterns patterns requiring odd sides core assembly patterns |
| Moulds include one (1) or more of the following: | undercut/drawback irregular/uneven jointed multi-part moulds |
| Cores include one (1) or more of the following: | full half segment |
| Mould securing methods include one (1) or more of the following: | weights clamps bolting |
| Moulding media includes one (1) or more of the following: | green sand shell sand chemically bonded media |
| Pouring basins include one (1) or more of the following: | hand pattern formed |
| Parting and stripping systems include one (1) or more of the following: | dry wet |

# Unit Mapping Information

Release 2. Supersedes and is equivalent to MEM04025 Produce moulds and cores by hand (advanced) (Release 1).

Release 1. Supersedes and is not equivalent to MEM04005C Produce moulds and cores by hand (jobbing).

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2

Assessment Requirements for MEM04025 Produce moulds and cores by hand (advanced)

# Modification History

Release 2. Quantum of hours of workplace practice removed. Supersedes and is equivalent to MEM04025 Produce moulds and cores by hand (advanced) (Release 1).

Release 1. Supersedes and is not equivalent to MEM04005C Produce moulds and cores by hand (jobbing).

# Performance Evidence

Evidence required to demonstrate competence in this unit must be relevant to and satisfy the requirements of the elements and performance criteria on at least two (2) occasions and include:

following work instructions, standard operating procedures (SOPs) and safe work practices

planning the production of moulds and cores by hand, including identifying job requirements and materials from drawings, instructions or specifications, job set up, and sequence operations for maximum safety and efficiency

assembling pattern to specification, including selecting, inspecting and setting up pattern equipment to conformance and identifying damaged patterns for repair or replacement

preparing to produce moulds and cores by positioning core in prints utilising chaplets and chills and vent to specification, closing mould, selecting and positioning appropriate moulding/core making equipment, selecting appropriate moulding media and securing mould

producing mould and core by selecting or manufacturing a pouring basin, ramming mould and cores with irregular joints and drawbacks, using parting and stripping systems, positioning and securing loose pieces, vents, risers and runners, and removing pattern and loose pieces from mould and core box

inspecting, cleaning, repairing and painting mould according to specification

disposing of unwanted treated sand according to SOPs

completing all proformas and standard workplace forms as required.

# Knowledge Evidence

Evidence required to demonstrate the required knowledge for this unit must be relevant to and satisfy the requirements of the elements and performance criteria and include knowledge of:

safe work practices and procedures and use of personal protective equipment (PPE)

metal casting process

variety of pattern types and their application in a casting process

pattern assembly techniques

procedures for selecting a moulding box to match job and pattern

principles and processes for selection of ancillary components

sand types and their bonding systems

compaction processes

parting and stripping systems

mould requirements including vents, runners, risers and other methoding requirements

finishing and closing techniques

core placement

pouring requirements

securing systems

pattern care and storage

environmental requirements.

# Assessment Conditions

Assessors must:

have vocational competency in producing moulds and cores by hand (jobbing) at least to the level being assessed with relevant industry knowledge and experience

satisfy the assessor requirements in the Standards for Registered Training Organisations 2015 or its replacement and comply with the National Vocational Education and Training Regulator Act 2011, its replacement or equivalent legislation covering VET regulation in a non-referring state/territory as the case requires.

Assessment must occur in a functioning workplace. Where assessment in the workplace would be unsafe, impractical or threatens the environment, assessment must occur in a sufficiently rigorous simulated environment that reflects the circumstances that would be experienced in a functioning workplace. Assessment must cover all aspects of workplace performance, including task skills, task management skills, contingency management skills and job role environment skills.

Conditions for assessment must include access to all tools, equipment, materials and documentation required, including relevant workplace procedures, product and manufacturing specifications.

Assessment processes and techniques must be appropriate to the language, literacy and numeracy requirements of the work being performed and the needs of the candidate.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2