# MEM06009 Hand forge complex shapes

Release: 1

MEM06009 Hand forge complex shapes

# Modification History

Release 1. Supersedes and is equivalent to MEM06009A Hand forge complex shapes

# Application

This unit of competency defines the skills and knowledge required to produce intricate solid forged shapes commonly forged in the forging and fabrication areas of industry.

It covers hand forging of different metals, using specialised techniques, tools and jigs where specialised methods of holding, positioning and lifting complex forgings are required.

Where hand forging of simple shapes is required unit MEM06001 Perform hand forging should also be selected.

Where the interpretation of technical drawings is required unit MEM09002 Interpret technical drawing should also be selected.

Where the selection and use of engineering measurement is required unit MEM12023 Perform engineering measurements should also be selected.

Where the selection and use of tools is required unit MEM18001 Use hand tools and unit MEM18002 Use power tools/hand held operations, should also be selected as appropriate.

No licensing, legislative or certification requirements apply to this unit at the time of publication.

Band:	A

Unit Weight:	4

# Pre-requisite Unit

| MEM06001 | Perform hand forging |
| --- | --- |
| MEM11011 | Undertake manual handling |
| MEM13015 | Work safely and effectively in manufacturing and engineering |
| MEM16006 | Organise and communicate information |

# Competency Field

Forging

# Elements and Performance Criteria

| Elements describe the essential outcomes. |  | Performance criteria describe the performance needed to demonstrate achievement of the element. |  |
| --- | --- | --- | --- |
| 1 | Determine job requirements | 1.1 | Follow standard operating procedures (SOPs) |
|  |  | 1.2 | Comply with work health and safety (WHS) requirements at all times |
|  |  | 1.3 | Use appropriate personal protective equipment (PPE) in accordance with SOPs |
|  |  | 1.4 | Identify job requirements from specifications, sketches, job sheets or work instructions |
| 2 | Forge complex shapes using hand tools on an anvil | 2.1 | Calculate material volume, making allowances for bending, material shrinkage and oxidisation, as required |
|  |  | 2.2 | Produce complex shapes using appropriate hand tools, procedures and techniques |
|  |  | 2.3 | Check forging to ensure conformance to tolerances and specifications |
| 3 | Perform splitting and bundling on anvil | 3.1 | Select and use appropriate tools and equipment |
|  |  | 3.2 | Apply hand forging techniques and procedures to forging and opening bundled and split sections making allowance for material shrinkage, distortion and oxidisation |
|  |  | 3.3 | Apply heat and control in specified areas of the material to be forged in accordance with SOPs |
|  |  | 3.4 | Handle forgings in a safe and correct manner |
|  |  | 3.5 | Check forgings to ensure conformance to tolerances and specifications |
| 4 | Produce jigs and tools for complex shapes | 4.1 | Select tools and equipment required to taper and bend materials appropriate to task requirements |
|  |  | 4.2 | Apply techniques for producing jigs and tools to specifications |
|  |  | 4.3 | Bend and shape jigs and patterns to requirements |
|  |  | 4.4 | Forge hand held tools to the cut pattern in accordance with specifications |
|  |  | 4.5 | Perform final shaping, heat treatment and sharpening to specifications |

# Foundation Skills

This section describes those required skills (reading, writing, oral communication and numeracy) that are essential to workplace performance in this unit of competency.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Range of Conditions

| This field allows for different work environments and conditions that may affect performance. Essential operating conditions that may be present (depending on the work situation, accessibility of the item, and local industry and regional contexts) are included. |  |
| --- | --- |
| Complex hand forging includes one (1) or more of the following: | shaping reverse tapering jump up section for bends |
| Hand forging techniques include one (1) or more of the following: | spreading surface chasing hot splitting |
| Equipment includes one (1) or more of the following: | diesel electric and gas furnaces coke fires gaseous oxygen/fuel equipment |

# Unit Mapping Information

Release 1. Supersedes and is equivalent to MEM06009A Hand forge complex shapes

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2

Assessment Requirements for MEM06009 Hand forge complex shapes

# Modification History

Release 1. Supersedes and is equivalent to MEM06009A Hand forge complex shapes

# Performance Evidence

Evidence required to demonstrate competence in this unit must be relevant to and satisfy the requirements of the elements and performance criteria on at least two (2) occasions and include:

following work instructions, standard operating procedures (SOPs) and safe work practices

selecting and using measuring guides

calculating allowances for material volume, bending, shrinkage and oxidisation

selecting and using hand forging tools to forge complex shapes on anvil to meet specifications

forging open and bundled split sections safely using heating equipment, as required, to meet specifications

producing jigs and tools for complex shapes

performing heat treatment processes for forgings.

# Knowledge Evidence

Evidence required to demonstrate the required knowledge for this unit must be relevant to and satisfy the requirements of the elements and performance criteria and include knowledge of:

safe work practices and procedures and use of personal protective equipment (PPE)

forging hand tools and their applications

techniques and procedures for hand forging complex shapes

procedures for measuring forged articles and numerical operations and calculations/formulae for complex shapes

forging temperatures and heat specifications for multiple pieces

tools, techniques and equipment required to taper and bend materials

effects of material shrinkage and oxidisation on the dimensions of the forged article

methods of overcoming/allowing for the effects of shrinkage and oxidisation when hand forging articles

procedures for handling forgings

heating equipment and applications and appropriate heat treatment processes for forging different materials.

# Assessment Conditions

Assessors must:

have vocational competency in hand forging complex shapes at least to the level being assessed with relevant industry knowledge and experience

satisfy the assessor requirements in the Standards for Registered Training Organisations 2015 or its replacement and comply with the National Vocational Education and Training Regulator Act 2011, its replacement or equivalent legislation covering VET regulation in a non-referring state/territory as the case requires

Where possible assessment must occur in operational workplace situations. Where this is not possible or where personal safety or environmental damage are limiting factors, assessment must occur in a sufficiently rigorous simulated environment that reflects realistic operational workplace conditions. This must cover all aspects of workplace performance, including environment, task skills, task management skills, contingency management skills and job role environment skills

Conditions for assessment must include access to all tools, equipment, materials and documentation required, including relevant workplace procedures, product and manufacturing specifications

Assessment processes and techniques must be appropriate to the language, literacy and numeracy requirements of the work being performed and the needs of the candidate.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2