# Assessment Requirements for MEM07042 Undertake corrections and basic maintenance to aluminium extrusion dies and die support systems

Release: 1

Assessment Requirements for MEM07042 Undertake corrections and basic maintenance to aluminium extrusion dies and die support systems

# Modification History

Release 1. Supersedes and is equivalent to MEM07042A Undertake corrections and basic maintenance to aluminium extrusion dies and die support systems

# Performance Evidence

Evidence required to demonstrate competence in this unit must be relevant to and satisfy the requirements of the elements and performance criteria on at least two (2) occasions and include:

following work instructions, standard operating procedures (SOPs) and safe work practices

complying with work health and safety (WHS), regulatory requirements and risk management associated with extruder operation and die handling

relating intended changes to bearings, apertures, other die components and toolstack components to particular extrusion faults

adjusting metal flow using workshop machines, hand tools and hand held power tools to correct bearings

maintaining bearings and other die components to specification

identifying situations where die or other components must be either scrapped or returned to die manufacturer

supervising or conducting trial extrusions to verify corrections

reporting and documenting results of corrections.

# Knowledge Evidence

Evidence required to demonstrate the required knowledge for this unit must be relevant to and satisfy the requirements of the elements and performance criteria and include knowledge of:

safe work practices and procedures and use of personal protective equipment (PPE)

die technology:

construction:

solid dies

hollow dies

die support components

composition and characteristics of various die steels

die manufacturing process

nitriding process and purpose

extrusion design process and behaviour of typical shapes during extrusion

bearings:

shape and definition

bearing deflections

bearing wash

bearing choke where entrance to die aperture is wider than the exit angle

negative bearing (entrance is narrower than the exit angle) increases speed of flow

die support technology and common faults:

bolsters:

matching of dies to bolsters

typical faults in extrusions related to poor bolster selection or fit

backers:

softening

dishing

feeder plates:

tolerances too close can cause heat related surface defects on extrusions

tolerances not matched to bearings in die can cause shape loss

extrusion process:

shape behaviour of typical extrusion products

channel shapes and tongue movement faults and typical distortions and corrections

runout length variations and possible causes:

recycled and unevenly cooled billets

out of alignment die slides

bearings worn or polished unevenly

operator variables:

incorrect heat settings

incorrect selection of bolster for die

poor breakthrough management

principles of flow:

variation of flow speed through local details and thicknesses

variation across container diameter

variation due to length of bearing

speed of metal through die along with temperature determines how metal flow fills die

source and purpose of heating of:

billet

die

extrusion and extrusion created heat

surface defects and their causes:

die lines caused by roughness at surface edges, damaged bearing edges, bearing wash or flaking of nitriding

pick up (surface tearing)

streaking

blisters

inclusions in billets

nitriding flaking off die face

effects of incorrect heat:

collapsing of thin walled sections due to over heating

blocking of the die

surface breakdown and faults:

roughness

streaking

tearing

dangers of welding extrusion dies

die efficiency considerations:

monitor die performance over time using examine die and extrusion records

balance die correction against tonnage, speed and recovery rates

when to recommend new die or major re-work by die manufacturer where required.

# Assessment Conditions

Assessors must:

have vocational competency in undertaking corrections and basic maintenance to aluminium extrusion dies and die support systems at least to the level being assessed with relevant industry knowledge and experience

satisfy the assessor requirements in the Standards for Registered Training Organisations 2015 or its replacement and comply with the National Vocational Education and Training Regulator Act 2011, its replacement or equivalent legislation covering VET regulation in a non-referring state/territory as the case requires

Where possible assessment must occur in operational workplace situations. Where this is not possible or where personal safety or environmental damage are limiting factors, assessment must occur in a sufficiently rigorous simulated environment that reflects realistic operational workplace conditions. This must cover all aspects of workplace performance, including environment, task skills, task management skills, contingency management skills and job role environment skills

Conditions for assessment must include access to all tools, equipment, materials and documentation required, including relevant workplace procedures, product and manufacturing specifications

Assessment processes and techniques must be appropriate to the language, literacy and numeracy requirements of the work being performed and the needs of the candidate.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2