# MEM08006 Produce clear and/or coloured and/or sealed anodised films on aluminium

Release: 1

MEM08006 Produce clear and/or coloured and/or sealed anodised films on aluminium

# Modification History

Release 1. Supersedes and is equivalent to MEM08006B Produce clear and/or coloured and/or sealed anodised films on aluminium

# Application

This unit of competency defines the skills and knowledge required to produce clear or coloured sealed anodised films on aluminium and its alloys in applicable applications. Colouring is produced by dyeing or by ‘in-bath’ processes.

Where the interpretation of technical drawings is required unit MEM09002 Interpret technical drawing should also be selected.

Where the selection and use of engineering measurement is required unit MEM12023 Perform engineering measurements should also be selected.

Where the selection and use of tools is required unit MEM18001 Use hand tools and unit MEM18002 Use power tools/hand held operations, should also be selected as appropriate.

No licensing, legislative or certification requirements apply to this unit at the time of publication.

Band:	A

Unit Weight:	2

# Pre-requisite Unit

| MEM08002 | Pre-treat work for subsequent surface coating |
| --- | --- |
| MEM11011 | Undertake manual handling |
| MEM13015 | Work safely and effectively in manufacturing and engineering |
| MEM16006 | Organise and communicate information |

# Competency Field

Surface finishing

# Elements and Performance Criteria

| Elements describe the essential outcomes. |  | Performance criteria describe the performance needed to demonstrate achievement of the element. |  |
| --- | --- | --- | --- |
| 1 | Determine job requirements | 1.1 | Follow standard operating procedures (SOPs) |
|  |  | 1.2 | Comply with work health and safety (WHS) requirements at all times |
|  |  | 1.3 | Use appropriate personal protective equipment (PPE) in accordance with SOPs |
|  |  | 1.4 | Identify job requirements from specifications, job sheets or work instructions |
| 2 | Prepare for anodising | 2.1 | Apply taping and waxing masking techniques, where required |
|  |  | 2.2 | Minimise contact marks and shielding |
| 3 | Assess preparation of work for correct jigging/loading | 3.1 | Connect work correctly for the required current flow with minimum contact marks and shielding |
|  |  | 3.2 | Reject all incorrectly loaded work |
| 4 | Anodise work | 4.1 | Carry out anodising treatment steps following SOPs |
|  |  | 4.2 | Carry out sealing or dyeing and sealing steps following SOPs |
|  |  | 4.3 | Maintain process parameters within specified limits |

# Foundation Skills

This section describes those required skills (reading, writing, oral communication and numeracy) that are essential to workplace performance in this unit of competency.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Range of Conditions

| This field allows for different work environments and conditions that may affect performance. Essential operating conditions that may be present (depending on the work situation, accessibility of the item, and local industry and regional contexts) are included. |  |
| --- | --- |
| Applications include one (1) or more of the following: | electrical decorative mechanical architectural purposes |
| Anodising steps include (1) one or more of the following: | pre treatment anodising dyeing sealing |
| Masking techniques include one (1) or more of the following: | taping waxing |
| Process parameters include one (1) or more of the following: | temperature current density time |

# Unit Mapping Information

Release 1. Supersedes and is equivalent to MEM08006B Produce clear and/or coloured and/or sealed anodised films on aluminium

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2