# MEM08018 Electroplate engineering coatings

Release: 1

MEM08018 Electroplate engineering coatings

# Modification History

Release 1. Supersedes and is equivalent to MEM08018B Electroplate engineering coatings

# Application

This unit of competency defines the skills and knowledge required to apply engineering metallic/ceramic coatings to ferrous and non-ferrous metals and some non-metallic materials, e.g. plastics.

It applies to producing engineering coatings designed to promote wear resistance, protect against corrosion, and reclaim worn components. It also applies to manufacturing components (electroforming).

Where pre-treatment operations only are required unit MEM08002 Pre-treat work for subsequent surface coating should be selected.

Where straightforward operation of electroplating process is required unit MEM08003 Perform electroplating operations should be selected.

Where surface preparation operations are required unit MEM08011 Prepare surfaces using solvents and/or mechanical means and unit MEM08012 Prepare surfaces by abrasive blasting (basic), should also be selected as appropriate.

Where the interpretation of technical drawings is required unit MEM09002 Interpret technical drawing should also be selected.

Where the selection and use of engineering measurement is required unit MEM12023 Perform engineering measurements should also be selected.

Where basic inspection of completed or partly completed products produced by others is required unit MEM15004 Perform inspection should also be selected.

Where the selection and use of power tools/hand held operations is required unit MEM18002 Use power tools/hand held operations should also be selected.

Where construction of anodes, shields/robbers is required appropriate fabrication units should also be selected.

Where dogging/lifting is required appropriate materials handling units to suit regulatory requirements should also be selected.

No licensing, legislative or certification requirements apply to this unit at the time of publication.

Band:	A

Unit Weight:	6

# Pre-requisite Unit

| MEM07001 | Perform operational maintenance of machines/equipment |
| --- | --- |
| MEM08001 | Perform wire, jig and barrel load/unload work |
| MEM08003 | Perform electroplating operations |
| MEM11011 | Undertake manual handling |
| MEM13003 | Work safely with industrial chemicals and materials |
| MEM13015 | Work safely and effectively in manufacturing and engineering |
| MEM16006 | Organise and communicate information |
| MEM18001 | Use hand tools |

# Competency Field

Surface finishing

# Elements and Performance Criteria

| Elements describe the essential outcomes. |  | Performance criteria describe the performance needed to demonstrate achievement of the element. |  |
| --- | --- | --- | --- |
| 1 | Determine job requirements | 1.1 | Follow standard operating procedures (SOPs) |
|  |  | 1.2 | Comply with work health and safety (WHS) requirements at all times |
|  |  | 1.3 | Use appropriate personal protective equipment (PPE) in accordance with SOPs |
|  |  | 1.4 | Identify job requirements from specifications, job sheets or work instructions |
| 2 | Select treatments and processes/ equipment for producing engineering finishes | 2.1 | Select appropriate treatment processes according to base metal type, the surface condition and relevant job specifications |
|  |  | 2.2 | Select operating/process parameters to achieve required coating |
|  |  | 2.3 | Select appropriate equipment, as required |
| 3 | Prepare work for engineering finishes | 3.1 | Mask (stop off) products for selective plating |
|  |  | 3.2 | Construct conforming anodes and fit, where applicable |
|  |  | 3.3 | Construct and fit shields and robbers, where applicable |
|  |  | 3.4 | Carry out pre-treatment processes, where necessary |
| 4 | Monitor and control operating conditions and processes for engineering coatings | 4.1 | Set operating/process parameters to produce required surface conditions/specifications |
|  |  | 4.2 | Monitor and confirm surface conditions of finished components and identify abnormalities |
|  |  | 4.3 | Take corrective actions to rectify non-conforming conditions |
| 5 | Maintain solutions for engineering finishes | 5.1 | Check solution compositions and confirm to specification/operating range |
|  |  | 5.2 | Determine adjustment requirements/additions |
|  |  | 5.3 | Make additions to adjust solution composition to correct operating range as necessary |

# Foundation Skills

This section describes those required skills (reading, writing, oral communication and numeracy) that are essential to workplace performance in this unit of competency.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Range of Conditions

| This field allows for different work environments and conditions that may affect performance. Essential operating conditions that may be present (depending on the work situation, accessibility of the item, and local industry and regional contexts) are included. |  |
| --- | --- |
| Treatment processes include one (1) or more of the following: | electroplating electroforming electroless plating |
| Operating/process parameters include one (1) or more of the following: | treatment times and currents bath pH temperatures and densities anode conditions addition agent content cleanliness of contacts make-up maintenance of solution levels and purity |
| Coating includes one (1) or more of the following: | hard chroming heavy nickel electroless nickel nickel composites heavy deposits of nickel, copper and bronze up to 10 mm |
| Equipment includes one (1) or more of the following: | wire racks handling equipment barrels jigs shields robbers |
| Products include one (1) or more of the following: | Base materials, including: cast iron brass steels with machine welded sections |
| Masking materials include one (1) or more of the following: | wax lacquers tapes foils |
| Anodes include one (1) or more of the following: | soluble insoluble auxiliary anodes |
| Solution compositions include one (1) or more of the following: | cleaning pickling electroplating chromate acid dips |
| Checks include one (1) or more of the following: | density titration pH |
| Adjustment includes one (1) or more of the following: | strength of solutions temperature range |

# Unit Mapping Information

Release 1. Supersedes and is equivalent to MEM08018B Electroplate engineering coatings

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2