# MEM24010 Perform radiographic testing

Release: 1

MEM24010 Perform radiographic testing

# Modification History

Release 1. Supersedes and is equivalent to MEM24010B Perform radiographic testing.

# Application

This unit of competency defines the skills and knowledge required to operate radiographic testing equipment in a range of industrial applications including fabrications, structures and components across a wide range of industries to Level 2 (AS 3669 Non-destructive testing – Qualification and approval of personnel – Aerospace and AS ISO 9712 Non-destructive testing — Qualification and certification of NDT personnel) or equivalent.

Radiographic tests are performed on critical component or structural zones., Re-assessment of competency may be required at regular intervals in accordance with Australian Standards or other relevant standards. Actual and potential defects are to be considered, together with ongoing abnormalities.

All testing must be completed with particular attention to personal and work health and safety (WHS) regulations and ionizing radiation equipment materials and chemicals, which are subject to codes and regulations, must be stored, used, and transported in accordance with safe work practices.

Where interpretation of technical drawings is required unit MEM09002 Interpret technical drawing should also be selected.

Where the selection and use of engineering measurement is required unit MEM12023 Perform engineering measurements should also be selected.

Where the selection and use of power tools are required unit MEM18002 Use power tools/hand held operations should also be selected.

No licensing or legislative requirements apply to this unit at the time of publication. Certification against Australian Standards may be achieved where assessment in this unit of competency is carried out in conjunction with an examining authority as described in AS ISO 9712 Non-destructive testing — Qualification and certification of NDT personnel.

#### Band: B

#### Unit Weight: 6

# Pre-requisite Unit

MEM11011 Undertake manual handling

MEM13018 Work safely with ionizing radiation

MEM13015 Work safely and effectively in manufacturing and engineering

MEM16006 Organise and communicate information

MEM18001 Use hand tools

MEM24012 Apply metallurgical principles

# Competency Field

Non-destructive testing

# Unit Sector

# Elements and Performance Criteria

| Elements | Performance Criteria |
| --- | --- |
| Elements describe the essential outcomes. | Performance criteria describe the performance needed to demonstrate achievement of the element. |
| 1. Determine job requirements | 1.1 Follow standard operating procedures (SOPs) 1.2 Comply with WHS requirements at all times 1.3 Use appropriate personal protective equipment (PPE) in accordance with SOPs 1.4 Identify job requirements from specifications |
| 2. Prepare inspection areas for radiographic testing | 2.1 Identify inspection area and clean and prepare for testing using appropriate procedures and materials 2.2 Carry out preparation processes in accordance with the relevant procedures and statutory requirements 2.3 Assess inspection areas visually and identify obvious discontinuities |
| 3. Select and prepare radiographic test | 3.1 Select the most appropriate radiographic test for the material and/or application 3.2 Select appropriate testing and processing equipment and set up for various geometrise in accordance with standards and/or procedures 3.3 Optimise quality of radiographic test |
| 4. Perform tests and maintain equipment | 4.1 Carry out radiographic tests in accordance with relevant standards, codes and specifications 4.2 Set up radiographs and carry out for specialised applications 4.3 Process films to maximise quality of image and achieve optimum results 4.4 Check radiographic testing equipment for defects and maintain and store in accordance with procedures and manufacturer instructions |
| 5. Monitor and ensure radiation safety | 5.1 Set up and maintain safety controls 5.2 Minimise radiation exposure to employees and general public 5.3 Select radiation monitoring equipment and use |
| 6. Interpret and report the results of radiographic tests | 6.1 Establish conditions necessary to view and interpret radiographs 6.2 Interpret and evaluate radiographs in accordance with applicable codes, standards and specifications 6.3 Report test results in accordance with organisational procedures, accepted industry practices and customer service requirements |

# Foundation Skills

This section describes those language, literacy, numeracy and employment skills that are essential to performance.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Range of Conditions

| This field allows for different work environments and conditions that may affect performance. Essential operating conditions that may be present (depending on the work situation, needs of the candidate, accessibility of the item, and local industry and regional contexts) are included. |  |
| --- | --- |
| Preparation processes include: | surface cleaning and drying. |

# Unit Mapping Information

Release 1. Supersedes and is equivalent to MEM24010B Perform radiographic testing.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2

Assessment Requirements for MEM24010 Perform radiographic testing

# Modification History

Release 1. Supersedes and is equivalent to MEM24010B Perform radiographic testing.

# Performance Evidence

Evidence required to demonstrate competence in this unit must be relevant to and satisfy the requirements of the elements and performance criteria and include:

following work instructions, standard operating procedures (SOPs) and safe work practices

identifying and interpreting specifications, relative testing and conformance standards for performing radiographic testing

preparing the area for testing and identifying discontinuities in accordance with procedures

applying safety practices and controls for minimising radiation exposure including effectively designing exposure and storage areas and calculating shielding thickness in accordance with procedures

carrying out radiographic testing using techniques and equipment appropriate for material/s to be tested, calculating and producing optimum quality radiographs on at least two occasions

interpreting and evaluating radiographs in accordance with applicable codes, standards and specifications and documenting and reporting test results in accordance with procedures and customer service requirements on at least two occasions.

Note: Where a volume and/or frequency is not specified, demonstration must be provided at least once.

# Knowledge Evidence

Evidence required to demonstrate the required knowledge for this unit must be relevant to and satisfy the requirements of the elements and performance criteria and include knowledge of:

safe work practices and procedures and use of personal protective equipment (PPE)

cleaning and preparation processes for test surfaces

assessment procedures and techniques

types of discontinuities and their effect on the material

procedures for carrying out each radiographic test and for specialised radiographic applications

principal types of X-ray generators and radioisotopes and their effect on radiographic sensitivity

tools, equipment, techniques and system verification checks

relevant standards, regulations and codes

principles of image formation, film and chemical properties and processing techniques

various types of films and screens, their properties and effects on image quality

maintenance and storage procedures for test equipment

common faults and damage

safety features of radioisotope cameras and X-ray equipment

production of X-rays and gamma rays and comparison of them on basis of energy and intensity

absorption of ionizing radiation by matter and the biological effects on living

X-ray equipment

gamma ray sources

shielding thickness

exposure calculations and techniques

reciprocity law

preparation and use of exposure charts and radiographic equivalence charts

equipment types and set-up procedures

types of materials and industrial applications

methods and/or procedures for reporting test results

implications of test results for the particular material and or application

the following defects:

corrosion

metal fatigue

deformation in nonferrous alloys, ferrous alloys and steels

composite materials

fatigue cracks

stress corrosion cracking

manufacturing defects

thickness measurement and fit

mechanical and bonded repairs

welding defects

casting defects.

# Assessment Conditions

Assessors must:

have vocational competency in performing radiographic testing at least to the level being assessed with relevant industry knowledge and experience

satisfy the assessor requirements in the Standards for Registered Training Organisations 2015 or its replacement and comply with the National Vocational Education and Training Regulator Act 2011, its replacement or equivalent legislation covering VET regulation in a non-referring state/territory as the case requires.

Where possible, assessment must occur in operational workplace situations. Where this is not possible or where personal safety or environmental damage are limiting factors, assessment must occur in a sufficiently rigorous simulated environment that reflects realistic operational workplace conditions that cover all aspects of workplace performance, including environment, task skills, task management skills, contingency management skills and job role environment skills.

Conditions for assessment must include access to all tools, equipment, materials and documentation required including relevant workplace procedures, product and manufacturing specifications.

Assessment processes and techniques must be appropriate to the language, literacy and numeracy requirements of the work being performed and the needs of the candidate.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2