# MEM48021 Apply metallurgical principles and techniques in welding and other thermal processes

Release: 1

MEM48021 Apply metallurgical principles and techniques in welding and other thermal processes

# Modification History

Release 1. Supersedes and is equivalent to MSATCM510A Apply metallurgical principles and techniques in welding and other thermal processes.

# Application

This unit of competency defines the skills and knowledge required to apply metallurgical principles and techniques to welding applications as a member of a design and development team or similar in support of the design and development of welding and other thermal practices in mechanical and manufacturing applications.

No licensing, legislative or certification requirements apply to this unit at the time of publication.

# Pre-requisite Unit

MEM09229 Read and interpret technical engineering drawings

MEM30007 Select common engineering materials

MEM48011 Apply basic chemical principles to metallurgy

MEM48012 Calculate and predict chemical outcomes in metallurgical situations

MEM48016 Select metal joining process

# Competency Field

Metallurgy

# Elements and Performance Criteria

| Elements | Performance Criteria |
| --- | --- |
| Elements describe the essential outcomes. | Performance criteria describe the performance needed to demonstrate achievement of the element. |
| 1. Determine job requirements | 1.1 Follow standard operating procedures (SOPs) 1.2 Comply with work health and safety (WHS) requirements at all times 1.3 Undertake consultations and briefings with managers, employers and customers to determine welding application requiring metallurgical specification and analysis |
| 2. Select welding or thermal process principles and techniques | 2.1 Conduct consultations, briefings and research to determine welding application, metallurgical specification and analysis required 2.2 Select relevant welding and thermal cutting techniques, principles and associated technologies for application |
| 3. Undertake welding and thermal process analysis and specify welding or other thermal process solutions | 3.1 Apply relevant scientific principles in a consistent and appropriate manner to obtain the required welding or thermal process solution 3.2 Use appropriate calculations and coherent units in the solution of engineering calculations 3.3 Use significant figures in engineering calculations 3.4 Apply techniques and associated technologies, software and hardware to obtain the required welding or thermal process solutions 3.5 Report analysis results and recommend welding or thermal process solution |

# Foundation Skills

This section describes those language, literacy, numeracy and employment skills that are essential to performance.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Range of Conditions

| This field allows for different work environments and conditions that may affect performance. Essential operating conditions that may be present (depending on the work situation, needs of the candidate, accessibility of the item, and local industry and regional contexts) are included. |  |
| --- | --- |
| Sources of information include one or more of the following: | reference standards and texts manufacturer catalogues and industrial magazines websites phone information gathering email information gathering. |
| Welding defects include: | shape defects including: excess weld metal overlap undercut lack of fusion and penetration including: incomplete root penetration lack of root fusion lack of interrun fusion lack of side wall fusion inclusions including: linear isolated oxides gas porosity including: worm hole uniform restart surface solidification porosity including: crater pipe shrinkage porosity solidification cracking including: hot cracking lamellar tearing weldability of aluminium and its alloys including: inherent problems including: hydrogen porosity oxide their prevention hot cracking including: causes alloys susceptible alloys resistant filler metals weldability of carbon and low steels and the welding zones of steel including: identification and microstructures relation to the iron or iron carbide equilibrium diagram multi-run welds cold cracking including: effects of hydrogen martensite stress austenitic stainless steels including: hot cracking corrosion intergranular corrosion heat affected zone precipitation carbide stabilisers extra low carbon stainless. |
| Other thermal processes include one or more of the following cutting, gouging, shaping or local treatment processes: | oxyacetylene oxyhydrogen plasma carbon arc. |

# Unit Mapping Information

Release 1. Supersedes and is equivalent to MSATCM510A Apply metallurgical principles and techniques in welding and other thermal processes.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2

Assessment Requirements for MEM48021 Apply metallurgical principles and techniques in welding and other thermal processes

# Modification History

Release 1. Supersedes and is equivalent to MSATCM510A Apply metallurgical principles and techniques in welding and other thermal processes.

# Performance Evidence

Evidence required to demonstrate competence in this unit must be relevant to and satisfy the requirements of the elements and performance criteria and include:

following work instructions, standard operating procedures (SOPs) and safe work practices

undertaking consultations with relevant personnel and researching other sources of information including industry codes and standards in applying metallurgical principles and techniques to welding and other thermal practices appropriate to the application

selecting appropriate scientific principles to suit specific welding applications on at least two occasions

selecting appropriate basic mechanical techniques and associated technologies, software and hardware to suit required applications in welding

applying and manipulating appropriate formulas for applications involving engineering calculations

applying appropriate calculations to engineering situations

referring solutions to the original aim of the welding application

quoting solutions in appropriate units using appropriate significant figures

quoting limitations of solutions due to assumptions, scientific principles and techniques used

reporting test results and presenting and recommending welding or thermal process solution.

Note: Where a volume and/or frequency is not specified, demonstration must be provided at least once.

# Knowledge Evidence

Evidence required to demonstrate the required knowledge for this unit must be relevant to and satisfy the requirements of the elements and performance criteria and include knowledge of:

safe work practices and procedures

sources of information

welding principles and processes including:

mechanical

electrical chemical

metallurgical processes associated with welding

limitations of scientific principles associated with welding

weld defect description including for C-Mn and low alloy steels

shape defects

lack of fusion and penetration

inclusions

gas porosity

solidification porosity

solidification cracking

hydrogen heat-affected zone cracking

reheat cracking

weldability of aluminium and its alloys

hot cracking

heat affected zone cracking

welding age-hardened alloys

welding work-hardened alloys

weldability of carbon and low steels and the welding zones of steel

hot cracking including carbon-manganese and sulphur ratio

cold cracking

calculation of carbon equivalents

hydrogen content of steel welds and its control

residual stress avoidance and removal

calculation of weld pre-heat temperatures

tests for cold crack susceptibility

weldability of stainless steels and stainless-steel types

thermal and electrical conductivity

thermal expansion

Schaeffler and Delong diagrams to predict structures

austenitic stainless steels

other special grades

weldability of cast irons

special techniques

weldability of the nickel alloys

filler metals and braze welding

other thermal processes including:

cutting

gouging

shaping.

# Assessment Conditions

Assessors must:

have vocational competency in applying metallurgical principles and techniques in welding and other thermal processes at least to the level being assessed with relevant industry knowledge and experience

satisfy the assessor requirements in the Standards for Registered Training Organisations 2015 or its replacement and comply with the National Vocational Education and Training Regulator Act 2011, its replacement or equivalent legislation covering VET regulation in a non-referring state/territory as the case requires.

Where possible, assessment must occur in operational workplace situations. Where this is not possible or where personal safety or environmental damage are limiting factors, assessment must occur in a sufficiently rigorous simulated environment that reflects realistic operational workplace conditions that cover all aspects of workplace performance, including environment, task skills, task management skills, contingency management skills and job role environment skills.

Conditions for assessment must include access to all tools, equipment, materials and documentation required including relevant workplace procedures, product and manufacturing specifications.

Assessment processes and techniques must be appropriate to the language, literacy and numeracy requirements of the work being performed and the needs of the candidate.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=b7050d37-5fd0-4740-8f7d-3b7a49c10bb2