# Assessment Requirements for MSFGG2014 Cut thin glass by hand

Release: 1

Assessment Requirements for MSFGG2014 Cut thin glass by hand

# Modification History

Release 1. Supersedes and is not equivalent to MSFGG2004 Process thin glass by hand.

# Performance Evidence

There must be evidence the candidate has completed the tasks outlined in the elements and performance criteria of this unit, and:

undertaken the following in accordance with all safety requirements and Australian Standard AS/NZS 4667:

for annealed glass, up to 8mm in thickness and up to 1.0 m 2in size, cut all of the following both in a thickness up to 6mm and in a thickness 6mm or above:

freehand cuts using templates for simple shapes other than square

straight cuts by hand and speed cutter

truncated and radius corners

circles

fan holes

freehand pay holes

for laminated glass, up to 8.38 mm in thickness and up to 1.0 m 2in size, cut all of the following at least once:

simple shapes other than a square

truncated corners

ovals

made straight cuts in laminated glass up to 8.38mm by hand and speed cutter.

# Knowledge Evidence

There must be evidence the candidate has knowledge of:

purpose and key provision of Australian Standard AS/NZS 4667 – all sections

work flow requirements in relation to glass cutting

mathematical procedures for estimation and measurement, including calculation of area and estimation of glass requirements

thin glass:

qualities and characteristics, including hazards and handling requirements

workplace safety system requirements

work flow requirements

common work requirements, including:

cut types

shaping

holes

edges

how to create a template for cutting

types, characteristics, safe use, maintenance and limitations of glass cutting tools and equipment, including:

cutters, including circle, speed, tungsten wheel

cutting tables

templates

cutting and processing techniques, the types of problems that may occur and how to avoid and respond

quality assurance

workplace documentation requirements.

# Assessment Conditions

Skills must have been demonstrated in the workplace or in a simulated environment that reflects workplace conditions and contingencies. The following conditions must be met for this unit:

use of suitable facilities, equipment and resources, including:

equipment, tools and materials required to complete tasks specified in the Performance Evidence

glass product to be cut

safety and personal protective equipment

work orders

workplace procedures.

Assessors must satisfy the NVR/AQTF mandatory competency requirements for assessors.

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=0601ab95-583a-4e93-b2d4-cfb27b03ed73