# Assessment Requirements for MSL975010 Perform fire assay techniques

Release: 1

Assessment Requirements for MSL975010 Perform fire assay techniques

# Modification History

Release 1. Supersedes and is equivalent to MSL975010A Perform fire assay techniques

# Performance Evidence

Evidence of competence in this unit must satisfy all of the requirements of the elements and performance criteria, and include demonstration of:

safely performing fire assay techniques to extract a range of precious metals from their host matrices in readiness for analysis on at least three (3) occasions

interpreting and closely following standard recovery methods

selecting and modifying laboratory methods to suit particular ores and to ensure total recovery

accurately weighing samples and flux components

maintaining close attention to technical and safety requirements in a physically demanding hazardous environment

maintaining sequential control of samples through all recovery stages

optimising work flow to ensure efficiency of recovery for multiple client samples

recognising and identifying the cause of non-acceptable received and fused samples, buttons and prills

identifying indicators of poor recovery and contamination

applying knowledge of mineral chemistry and fire assay techniques to solve recovery and contamination problems

keeping accurate and complete records, including:

pour sheets (date, time, client, pour number and preparation method)

number of pots, positions of sample, blank and check in rack

adjustments made to standard preparation methods for specific samples

analytical method

assay data

minimising rework, waste and environmental impacts

safely collecting and disposing of all waste responsibly

recognising hazards, using workplace safety procedures and safety equipment to work safely at all times.

# Knowledge Evidence

Must provide evidence that demonstrates knowledge of:

chemical and physical principles relating to:

fusion of mineral ores

cupellation

parting and digestion processes

expected physical and chemical properties of materials at each recovery stage

standard methods for the fire assay of a range of precious metal ores relevant to job role

criteria for an 'acceptable' button, including:

one piece, mass >20g and <50g

malleable

separates cleanly from slag

free of undecomposed ore, matte and speiss

causes of contamination, including:

poorly made cupels

base metals (copper (Cu), nickel (Ni), zinc (Zn) and bismuth (Bi))

arsenic (As), sulphur (S), antimony (Sb), selenium (Se), tellurium (Te) and chromium (Cr)

scoria

sprouting

indicators of potential loss and the corrective actions, including:

viscous slag (check furnace temperature, adjust flux and lower charge weight)

lead shotting (adjust flux and lower charge weight to compensate for high oxides, silicates and chromites)

sulphides (adjust fusion time and adjust sample weight and/or flux)

matte, speiss (adjust sample weight and flux)

incomplete fusion (adjust sample weight and/or flux)

unacceptable button (adjust sample weight and/or flux)

inquartation (add 3 parts silver (Ag) to prill, wrap in lead foil and re-cupel)

workplace safety procedures and operation of safety equipment

function and operation of assay/equipment used as part of job role

workplace and/or legal traceability requirements

relevant hazards, work health and safety (WHS) and environment requirements.

# Assessment Conditions

Judgment of competence must be based on holistic assessment of the evidence. Assessment methods must confirm consistency of performance over time, rather than a single assessment event.

This unit of competency is to be assessed in the workplace or a simulated workplace environment. A simulated workplace environment must reflect realistic operational workplace conditions that cover all aspects of workplace performance, including the environment, task skills, task management skills, contingency management skills and job role environment skills.

Foundation skills are integral to competent performance of the unit and should not be assessed separately.

Assessment processes and techniques must be appropriate to the language, literacy and numeracy requirements of the work being performed and the needs of the candidate.

Knowledge evidence may be collected concurrently with performance evidence or through an independent process, such as workbooks, written assessments or interviews (provided a record is kept in each case).

This unit of competency may be assessed with:

MSL975020 Apply routine spectrometric techniques

Holistic assessment methods include:

observation of the candidate

review of quality control performance and analytical results traceable to assay samples prepared by the candidate

review of sample records prepared by the candidate

feedback from supervisors, peers and/or clients about the candidate’s ability to safely and efficiently extract a range of precious metals from their host matrices in readiness for analysis, provide acceptable buttons and prills, and troubleshoot and correct common recovery failures

written/oral questioning about relevant mineral chemistry principles, precious metal recovery steps, typical problems and corrective actions.

Access is required to instruments, equipment, materials, workplace documentation, procedures and specifications associated with this unit, including, but not limited to:

client requests/documentation, including client profile, sample identification, sample receipt, storage and analyses, and required preparation method/and service charges

a variety of precious metal ore samples

fire assay methods, examples of assay records, equipment, materials and reagents

assay equipment, including:

mixing equipment and balances

fusion and muffle furnaces and associated spares

temperature sensors and hotplates

compressed air service, extraction systems and fuel supply lines

pots, cupels, pouring equipment, pot loader, trolleys, moulds, tongs and hammers

safety equipment and workplace safety procedures.

Assessors must satisfy the assessor competency requirements that are in place at the time of the assessment as set by the VET regulator.

The assessor must demonstrate both technical competence and currency.

Technical competence can be demonstrated through:

relevant VET or other qualification/Statement of Attainment AND/OR

relevant workplace experience.

Currency can be demonstrated through:

performing the competency being assessed as part of current employment OR

having consulted with a laboratory about performing the competency being assessed within the last twelve months.

# Links

MSA Training Package Implementation Guides - http://mskills.org.au/training-packages/info/