# MSMPMC300 Produce structural precast concrete

Release: 1

MSMPMC300 Produce structural precast concrete

# Modification History

Release 1. New unit. Supersedes and is equivalent to PMC553051 Produce structural precast concrete

# Application

This unit describes the skills and knowledge required to produce structural precast and pre-stressed concrete products, including beams and girders.

This unit applies to experienced operators who are required to take responsibility for own outputs and follow established procedures to assemble moulds and reinforcement; mould, cure and strip the product and control quality. Operators are also required to work autonomously and apply their own judgement to interpret information; monitor processes; identify and address routine and non-routine problems and control hazards.

The unit applies to an experienced operator working alone or as part of a team or group and in liaison with other shift team members, team leader and supervisor.

No licensing or certification requirements exist at the time of publication. Relevant legislation, industry standards and codes of practice within Australia must be applied.

# Pre-requisite Unit

Nil

# Competency Field

Operations

# Elements and Performance Criteria

| Elements | Performance Criteria |
| --- | --- |
| Elements describe the essential outcomes. | Performance criteria describe the performance needed to demonstrate achievement of the element. |
| 1. Prepare mould for casting | 1.1 Check casting schedule and job specification 1.2 Clean and oil moulds according to requirements 1.3 Check for mould damage and repair |
| 2. Assemble reinforcement cage | 2.1 Lift preassembled reinforcing sections into mould safely 2.2 Assemble additional steel to complete cage to drawings and job specification 2.3 Fit additional items, including base plates, tie plates and lifting devices, according to work instructions 2.4 Fit hold-ups and hold-downs as appropriate 2.5 Place voids or ducts according to work specifications 2.6 Run pre-stressing strands through reinforcing cages 2.7 Set up guards and comply with WHS requirements for stressing 2.8 Tension strands to extension dimensions and/or gauge readings according to works or engineer instructions 2.9 Recheck reinforcing cage is in correct position and adjust as necessary |
| 3. Close mould and test vibrators | 3.1 Lift mould sides and additional parts into position and secure to specification 3.2 Fit any additional items 3.3 Seal mould 3.4 Fit vibrators to start positions 3.5 Test run before casting commences |
| 4. Pour concrete | 4.1 Begin casting in accordance with work instructions 4.2 Move vibrators and time vibration 4.3 Screed top surface flat in preparation for final finish 4.4 Patch product 4.5 Clean mould and worksite in accordance with WHS requirements |
| 5. Control concrete quality | 5.1 Test raw materials 5.2 Prepare test cylinders and samples 5.3 Monitor and control concrete mix to keep within specifications 5.4 Update all records and file all records and supplier certificates in appropriate place 5.5 Raise non-conformance reports |
| 6. Cure product | 6.1 Cover and cure mould and test cylinders in accordance with standard procedures and work instructions 6.2 Monitor curing to achieve specified stripping strength |
| 7. Strip and store product | 7.1 Test samples to ensure specific strength has been achieved 7.2 Remove mould sides and store ready for cleaning 7.3 De-stress in accordance with work procedures and sequences 7.4 Lift unit according to work instructions and move to store, supported only on points designated on the drawings |
| 8. Respond to problems | 8.1 Identify routine and non-routine problems in the equipment or process 8.2 Rectify problems using appropriate solution within area of responsibility 8.3 Report problems outside area of responsibility to designated person |
| 9. Control hazards | 9.1 Identify structural precast and pre-stressed concrete production hazards 9.2 Assess the risks arising from those hazards 9.3 Implement measures to control those risks |

# Foundation Skills

This section describes those required skills (language, literacy and numeracy) that are essential to performance.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Unit Mapping Information

Release 1. New unit. Supersedes and is equivalent to PMC553051 Produce structural precast concrete

# Links

Companion Volume Implementation Guides are available at VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=d1287d36-dff4-4e9f-ad2c-9d6270054027

Assessment Requirements for MSMPMC300 Produce structural precast concrete

# Modification History

Release 1. New unit. Supersedes and is equivalent to PMC553051 Produce structural precast concrete

# Performance Evidence

There must be evidence the candidate has completed the tasks outlined in the elements and performance criteria of this unit, and:

produced at least 1 structural precast concrete product, including:

monitoring the following key variables to ensure product integrity and conformance to specification:

mould condition

amount and consistency of concrete mix

placement and anchorage of reinforcement and fittings

placement of voids and ducts

tension of reinforcement

concrete cover

compaction and vibration

curing conditions

curing time and rate

stripping strength

recognising possible causes of the following routine problems:

raw material and mix variations

mould anomalies

casting and operating conditions

reinforcement abnormalities

process errors.

# Knowledge Evidence

There must be evidence the candidate has knowledge of:

principles of casting process

significance to structural concrete products of key factors, including:

concrete cover

role of reinforcement

placement and anchorage of reinforcement and fittings

stressing and destressing

curing

compaction and vibration

formwork and specialised formwork (including voids and ducts)

mould design

mould condition and wear

water and cement ratio

concrete finishing

methods of:

curing

compaction

fabrication

concrete sampling and testing procedures

the potential effects of variations in raw materials and equipment operation and processes in relation to quality of product

quality requirements at each stage of production

common adjustments in variables and their impact on product quality and production output

routine and non-routine problems, their probable causes and relevant corrective actions

hazards from critical stages of pre-stressing reinforcement (placement, stressing, de-stressing, cutting)

work health and safety (WHS) requirements relevant to work outcome

structural precast and pre-stressed concrete production hazards and:

their possible causes

potential consequences

risk control procedures.

# Assessment Conditions

Skills must have been demonstrated in the workplace or in a simulated environment that reflects workplace conditions and contingencies. The following conditions must be met for this unit:

use of suitable facilities, equipment and resources, including:

structural precast concrete equipment and ancillary equipment

materials to be processed

specifications, procedures and job sheets

modelling of industry operating conditions, including:

routine and non-routine problems.

Assessors must satisfy the NVR/AQTF mandatory competency requirements for assessors.

# Links

Companion Volume Implementation Guides are available at VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=d1287d36-dff4-4e9f-ad2c-9d6270054027