# MSMPMC330 Produce architectural precast concrete

Release: 1

MSMPMC330 Produce architectural precast concrete

# Modification History

Release 1. New unit. Supersedes and is equivalent to PMC553050 Produce architectural precast concrete

# Application

This unit describes the skills and knowledge required to produce architectural precast concrete products.

This unit applies to experienced operators who are required to take responsibility for own outputs and follow established procedures to prepare mould assemblies, fittings and reinforcement (not pre-stressed) and mould, cure and strip the product. Operators are also required to work autonomously and apply their own judgement to interpret information; monitor processes; identify and address routine and non-routine problems and control hazards.

The experienced operator may work alone or as part of a team or group and in liaison with other shift team members, team leader and supervisor.

No licensing or certification requirements exist at the time of publication. Relevant legislation, industry standards and codes of practice within Australia must be applied.

# Pre-requisite Unit

Nil

# Competency Field

Operations

# Elements and Performance Criteria

| Elements | Performance Criteria |
| --- | --- |
| Elements describe the essential outcomes. | Performance criteria describe the performance needed to demonstrate achievement of the element. |
| 1. Prepare mould for casting | 1.1 Check casting schedule, drawings and job specification 1.2 Check finish and veneer requirements for any or all faces, edges or surfaces 1.3 Prepare veneering equipment and formwork to temporarily support veneers and backing concrete |
| 2. Prepare reinforcement | 2.1 Check quantities, type, size and shape of reinforcement supplied against drawings and schedules 2.2 Place reinforcement and check concrete covers 2.3 Complete mould assembly 2.4 Insert lifting devices, lugs, fixing and other fittings according to drawings and specifications 2.5 Seal mould |
| 3. Cast concrete | 3.1 Pour concrete in correct sequence according to work schedule 3.2 Check adequate vibration 3.3 Complete casting process to plans and specification 3.4 Prepare test samples and/or cylinder as required by work instructions 3.5 Screed to a flat, accurate surface in preparation for finishing 3.6 Finish green concrete as required 3.7 Wet patch as required |
| 4. Cure product | 4.1 Cover and cure mould in accordance with standard procedure and any special requirements 4.2 Monitor curing to achieve specified stripping strength |
| 5. Strip and store product | 5.1 Safely remove mould parts at appropriate time, with care, and inspect for damage 5.2 Lift unit using appropriate lifting equipment and lifting methods 5.3 Arrange storage using protective pads to ensure against damage |
| 6. Respond to problems | 6.1 Identify routine and non-routine problems in the equipment or process 6.2 Rectify problems using appropriate solution within area of responsibility 6.3 Report problems outside area of responsibility to designated person |
| 7. Control hazards | 7.1 Identify architectural precast concrete production hazards 7.2 Assess the risks arising from those hazards 7.3 Implement measures to control those risks |

# Foundation Skills

This section describes those language, literacy, numeracy and employment skills that are essential to performance.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Unit Mapping Information

Release 1. New unit. Supersedes and is equivalent to PMC553050 Produce architectural precast concrete

# Links

Companion Volume Implementation Guides are available at VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=d1287d36-dff4-4e9f-ad2c-9d6270054027

Assessment Requirements for MSMPMC330 Produce architectural precast concrete

# Modification History

Release 1. New unit. Supersedes and is equivalent to PMC553050 Produce architectural precast concrete

# Performance Evidence

There must be evidence the candidate has completed the tasks outlined in the elements and performance criteria of this unit, and:

produced at least 1 architectural precast concrete product, including:

monitoring the following key variables to ensure product integrity and conformance to specification:

mould condition

amount and consistency of concrete mix

placement of reinforcement and fittings

concrete cover

compaction and vibration

curing conditions

curing time and rate

stripping strength

recognising possible causes of the following routine problems:

raw material and mix variations

mould anomalies

casting and operating conditions

process errors.

# Knowledge Evidence

There must be evidence the candidate has knowledge of:

principles of casting process

significance to architectural concrete products of key factors, including:

veneer adhesion

concrete cover

role of reinforcement

placement of reinforcement and fittings

curing

compaction and vibration

mould design

mould condition and wear

water-cement ratio

concrete finishing

methods of curing

compaction methods

fabrication methodologies

concrete sampling and testing procedures

the potential effects of variations in raw materials and equipment operation, processes in relation to quality of product

quality requirements at each stage of production

common adjustments in variables and their impact on product quality and production output

routine problems, their probable causes and relevant corrective actions

architectural precast concrete production hazards and:

their possible causes

potential consequences

risk control procedures.

# Assessment Conditions

Skills must have been demonstrated in the workplace or in a simulated environment that reflects workplace conditions and contingencies. The following conditions must be met for this unit:

use of suitable facilities, equipment and resources, including:

architectural precast concrete production equipment and ancillary equipment

materials to be processed

specifications, procedures and job sheets

modelling of industry operating conditions, including:

routine and non-routine problems.

Assessors must satisfy the NVR/AQTF mandatory competency requirements for assessors.

# Links

Companion Volume Implementation Guides are available at VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=d1287d36-dff4-4e9f-ad2c-9d6270054027