# PMBTECH301 Use material and process knowledge to solve problems

Release: 1

PMBTECH301 Use material and process knowledge to solve problems

# Modification History

Release 1. Supersedes and is equivalent to PMBTECH301B Use material and process knowledge to solve problems

# Application

This unit of competency covers the skills and knowledge required to apply material and process knowledge to solve problems.

This unit of competency applies to experienced operators who are required to recognise actual and potential process and product problems; identify the role of polymers, additives and other materials in the problems; and determine corrective action.

This unit of competency applies to an experienced operator demonstrating theoretical and technical knowledge and well developed skills in situations that require some discretion and judgement. The operator may work alone or as a member of a team or group and will work in liaison with other shift team members, team leader and supervisor, as appropriate.

No licensing, legislative or certification requirements apply to this unit at the time of publication.

# Pre-requisite Unit

Nil

# Competency Field

Technical

# Unit Sector

Not applicable

# Elements and Performance Criteria

| Elements describe the essential outcomes. |  | Performance criteria describe the performance needed to demonstrate achievement of the element. |  |
| --- | --- | --- | --- |
| 1 | Identify and apply applications of polymer materials | 1.1 | Identify typical applications for common polymer materials |
|  |  | 1.2 | Recognise physical properties of common polymers |
|  |  | 1.3 | Use additives with knowledge of the effects of using the incorrect amount/type of additive |
|  |  | 1.4 | Handle additives to minimise the associated risks |
| 2 | Identify and apply impacts of impurities on polymer products | 2.1 | Identify major impurities of concern to product and process |
|  |  | 2.2 | Examine polymer materials for impurities |
|  |  | 2.3 | Apply corrective actions to remove/compensate for impurities |
| 3 | Determine expected material properties from polymer type and grade | 3.1 | Identify the relationship between polymer type and polymer characteristics |
|  |  | 3.2 | Identify the relationship between polymer grade and degree of polymerisation |
|  |  | 3.3 | Identify the influence of polymer structure on properties |
| 4 | Solve process problems related to polymer flow characteristics | 4.1 | Use polymer flow test methods and recognise the importance of flow properties to the process |
|  |  | 4.2 | Control critical factors leading to changes of state of the polymer during processing using knowledge of the causes |
|  |  | 4.3 | Identify the relationship between polymer flow and other polymer properties |
|  |  | 4.4 | Recognise process/product signs of incorrect polymer flow characteristics |
|  |  | 4.5 | Recommend corrective actions for problems caused by polymer flow |
| 5 | Solve process/product problems related to heating and cooling of product/material in process | 5.1 | Recognise the importance of the degree of cross linking on product properties if appropriate |
|  |  | 5.2 | Recognise the importance of the degree of crystallisation/crystal size on product properties if appropriate |
|  |  | 5.3 | Recognise the impact of shrinkage on product properties if appropriate |
|  |  | 5.4 | Recognise the impact of annealing on product properties if appropriate |
|  |  | 5.5 | Recognise process/product signs of incorrect heating/cooling |
|  |  | 5.6 | Recommend corrective actions for problems caused by heating |
| 6 | Solve process problems related to polymer faults | 6.1 | Recognise an actual or a potential process problem |
|  |  | 6.2 | Analyse that problem in a formal manner |
|  |  | 6.3 | Determine appropriate corrective action |
|  |  | 6.4 | Implement that corrective action if it is within the range of workplace authority |
|  |  | 6.5 | Make recommendations for corrective action outside range of workplace authority |
|  |  | 6.6 | Follow through on corrective action and make sure problem is resolved |

# Foundation Skills

This section describes those required skills (language, literacy and numeracy) that are essential to performance.

Foundation skills essential to performance are explicit in the performance criteria of this unit of competency.

# Range of Conditions

| This field allows for different work environments and conditions that may affect performance. Essential operating conditions that may be present (depending on the work situation, needs of the candidate, accessibility of the item, and local industry and regional contexts) are included. |  |
| --- | --- |
| Regulatory framework | The latest version of all legislation, regulations, industry codes of practice and Australian/international standards, or the version specified by the local regulatory authority, must be used. Applicable legislation, regulations, standards and codes of practice include: health, safety and environmental (HSE) legislation, regulations and codes of practice relevant to the workplace, manual handling and hazardous materials Australian/international standards relevant to the materials being used and products being made any relevant licence and certification requirements. All operations to which this unit applies are subject to stringent HSE requirements, which may be imposed through state/territory or federal legislation, and these must not be compromised at any time. Where there is an apparent conflict between performance criteria and such requirements the legislative requirements take precedence. |
| Procedures | All operations must be performed in accordance with relevant procedures. Procedures are written, verbal, visual, computer-based or in some other form, and include one or any combination of: problem solving techniques emergency procedures work instructions standard operating procedures (SOPs) safe work method statements (SWMS) formulas/recipes batch sheets temporary instructions any similar instructions provided for the smooth running of the plant. |
| Hazards | Hazards must be identified and controlled. Identifying hazards requires consideration of: hazardous products and materials vapours or other atmospheric hazards interaction of polymers, additives and other materials with process variables other hazards that might arise. |

# Unit Mapping Information

Release 1. Supersedes and is equivalent to PMBTECH301B Use material and process knowledge to solve problems

# Links

Companion Volume implementation guides are found in VETNet - https://vetnet.gov.au/Pages/TrainingDocs.aspx?q=932aacef-7947-4c80-acc6-593719fe4090